## Slide 1
Presenter: Ramya Gurunathan
Advisor: Prof. G. Jeffrey Snyder
Special Thanks:
Dr. Riley Hanus for his mentorship
The Snyder Group
Department of Materials Science
Northwestern University
February 6, 2020
Phonon-Defect Interactions in Thermoelectric Materials
Notes: Check slide number!!!!

## Slide 2
Crystalline Defects Attenuate Heat in a Solid
Vacancy Scattering
Dislocation Scattering
Sun, B., Haunschild, G., Polanco, C. et al. Nature Mater 18, 136–140 (2019).
Boundary Scattering
Dong, H., Wen, B. & Melnik, R. Sci Rep 4, 7037 (2015)
Notes: Pop up separately? Too busy

## Slide 3
Primary Tool: Analytic Theory
Why?
Reveal general, underlying physics
Routine modelling of experimental data
Appropriate for study of long-ranged strain fields
Toberer, E. ﻿J. Mater. Chem., 21, 15843 (2001).
Notes: The primary tool I’ll turn to is analytic theory which I’ll try to motivate with a couple of examples. Firstly that simple physics-based models give us some guiding principles and sanity checks when interpreting simulation or experimental results. This toy 1D chain model for phonons shows the impact of increasing the number of atoms in a unit cell or period on dispersion. From this, we learn to anticipate a reduction in the average phonon group velocity as a result of this effect. Simple, analytic expressions are attractive for routine modelling of experimental data. So, as will be discussed more soon, thermal conductivity is often measured as a function of composition and this blue U-curve is an analytic model that captures the experimental data extremely well without fitting parameters. Finally, in this particular case, we are interested in understanding the scattering effects of strain fields around defects. Dislocations, for example, have long-ranged stress fields that decays as 1/r and therefore would require extremely large simulations to study directly.
Animate?

## Slide 4
Components of Lattice Thermal Conductivity ()
Notes: Heat is carried through a solid via electrons and lattice vibrations. For a periodic solid, these vibrational modes are well-described as plane wave, normal modes or phonons. This presentation will focus on the lattice component of the thermal conductivity. So, we can start with the Callaway expression for lattice thrmal conductivity. For a frequency interval d omega, the efficacy of thermal transport for phonons in this range is determined by the amount of heat they can transport, or the heat capacity, how quickly the phonons move through the lattice, and the time it can travel before it trips on, say an interstital defect, inducing a scattering event.

## Slide 5
Fermi’s Golden Rule: Scattering due to a Static Perturbation
T.-S. Choy, J. Naset, J. Chen, S. Hershfield, and C. Stanton. Bulletin of The American Physical Society, 45(1):L36 42, 2000
Scattering rate from state k:
Notes: This naturally leads to scattering theory, which can be approached using fermi’s golden rule. The transition probability form an incident to final phonon state (k to k’) is determined mainly by the strength of the coupling between the phonons and the energy perturbation in the lattice, in this case induced by a defect. That coupling strength is captured in the squared perturbation matrix element. Additionally, one will need to consider the conservation crtieria in a given transition. The delta function enforces the energy conservation criteria. The squared matrix element can then be averaged over all possible final phonon states, with this factor to suppress any non-resistive forward scattering processes where the final phonon equals the incident phonon. Finally the scattering rate, will be the number density of defects, and their scattering strength. Finally, it should depend on the number of available states to scatter into.

## Slide 6
Fermi’s Golden Rule: Scattering due to a Static Perturbation
Scattering rate from state k:
T.-S. Choy, J. Naset, J. Chen, S. Hershfield, and C. Stanton. Bulletin of The American Physical Society, 45(1):L36 42, 2000
Notes: This naturally leads to scattering theory, which can be approached using fermi’s golden rule. The transition probability form an incident to final phonon state (k to k’) is determined mainly by the strength of the coupling between the phonons and the energy perturbation in the lattice, in this case induced by a defect. That coupling strength is captured in the squared perturbation matrix element. Additionally, one will need to consider the conservation crtieria in a given transition. The delta function enforces the energy conservation criteria. The squared matrix element can then be averaged over all possible final phonon states, with this factor to suppress any non-resistive forward scattering processes where the final phonon equals the incident phonon. Finally the scattering rate, will be the number density of defects, and their scattering strength. Finally, it should depend on the number of available states to scatter into.

## Slide 7
Phonon-Point Defect Scattering
Gurunathan, R., Hanus, R., Dylla, M., Katre, A., Snyder, G.J. arXiv:1910.03654, 2019.
Gurunathan, R., Hanus, R., Snyder, G.J. (submitted) 2020.
Notes: At the start of my PhD, I was first take a deeper look into the current representation of phonon-point defect scattering. This was motivated by discrepancies in the literature discovered by alumni of the group as well as a general curiosity about why these models appear to work so well given the ostensibly limiting approximation it makes. For example this plot of Mg2Sn-Mg2Si solid solution shows excellent correspondence the Klemens prediction in blue alongside two experimental data sets as well as a first-principles prediction represented by the doted line.
The scattering potential due to a point defect is a combination of the change in mass, change in harmonic force constant, and local strain encompassed by the change in site radius at the defect site. However, since the change in force constant is not a direct measurable, the entire change in bonding is represented by the change in radius. In this case, the fitting parameter epsilon is introduced. It is often the case that the scattering due to mass contrast is the dominant effect, such that the strain term can be ignored… since defects inducing large amounts of strain would be energetically unfavorable. So, in these cases, the model does not include any fitting parameters, as in the Mg2Sn case.

## Slide 8
Phonon-Point Defect Scattering
Notes: Motivate looking into this topic
Show discrepancy data

## Slide 9
Klemens Closed-form Alloy Scattering Model
k + k’ = k’’ + G
Klemens, P. Phys. Rev. 119, (1960).
Disorder parameter:

## Slide 10
Klemens Closed-form Alloy Scattering Model
k + k’ = k’’ + G
Klemens, P. Phys. Rev. 119, (1960).
Disorder parameter:

## Slide 11
Two Approximations Discussed for Polyatomic Crystals
Klemens
Slack
Volume of unit cell
Defect Microstates:
Notes: So there are two approximations used on polyatomic lattices, and they appeared differetn. The monatomic lattice approximations involves summing all the atoms in the unit cell into a single, vibrating mass. The other is the virtual crystal approximation, in which each atom has the average mass and average bond strength of every atom in the crystal. These are the implied phonon dispersions for each, just to show that they may appear incompatible. The monatomic lattice will throw away phonon modes owing to the consolidation of atoms, while the virtusal crystaldoes not, but involves in a shrinking of the real space unit cell and increase in the brillouin zone.
Arrows or some way to show what’s going on with the two models
Show example of incorrect thermal conductivity predictions

## Slide 12
Recommended Treatment of Point Defect Scattering
Atomically averaged variance
Atomically averaged quantity, squared
Literature shows common inappropriate assignment of
Gurunathan, R., Hanus, R., Dylla, M., Katre, A., Snyder, G.J. arXiv:1910.03654, 2019.
Gurunathan, R., Hanus, R., Snyder, G.J. (submitted) 2020.
Notes: Figure out explanation of this….
Metnion/describe expressions for Gamma in the literature

## Slide 13
Off-Stoichiometric Defect Scattering
Wang, Y., Li, F., et al. Inorganic Chemistry 50, 4412-4416 (2011)
Notes: Finally, we wanted to make a note about off-stoichiometric defects including bonds or interstitials. In this case, the perturbation induced by the defect comes from the kinetic energy change associated with a missing or added atom and the potential energy change associated with a missing or added bond. By the virial theorem, the time-averaged kinetic and potential energy on an atomic site are equal. Therefore, Since the potential energy perturbation due to a changei nbonding is twice the potential energy change per site, we get the relation v’ = 2t’, such that the full energy perturbation is just 3 times the mass perturbation generated by an added or substracted mass. This virial theorem argument is shown to work well for several experimental measurements of alloyed systems as shown below.
Animate
Experimentla data from lit, but my fits…. Show overprediction

## Slide 14
Off-Stoichiometric Defect Scattering
Interstitial Scattering
Vacancy Scattering
Pei, Y. et al. Adv. Electron. Mater. 2, 1600019 (2016).
Meisner, G. P. et al. Phys. Rev. Lett. 80, 3551–3554 (1998).
Wang, Y., Li, F., et al. Inorganic Chemistry 50, 4412-4416 (2011)
Notes: Finally, we wanted to make a note about off-stoichiometric defects including bonds or interstitials. In this case, the perturbation induced by the defect comes from the kinetic energy change associated with a missing or added atom and the potential energy change associated with a missing or added bond. By the virial theorem, the time-averaged kinetic and potential energy on an atomic site are equal. Therefore, Since the potential energy perturbation due to a changei nbonding is twice the potential energy change per site, we get the relation v’ = 2t’, such that the full energy perturbation is just 3 times the mass perturbation generated by an added or substracted mass. This virial theorem argument is shown to work well for several experimental measurements of alloyed systems as shown below.
Animate
Experimentla data from lit, but my fits…. Show overprediction

## Slide 15
Debye Approximation: Dispersion Dependence
Point Defect:
Umklapp:
Heat Capacity:
Debye
True
Notes: Contain a motif of the 3D density of states, through the phase space contribution of the final phonon states
It should be noted that the phase space in the Umklapp scattering term is not strictly equal to the density of states, as the phonon velocities may be defined at different phonon frequencies
Should be noted that the phase space contribution
Also, the form would be dispersion-dependent
Is the averaged v_g more similar to the v_s
Density of states

## Slide 16
Dispersion Dependence
Point Defect:
Umklapp:
Heat Capacity:
Notes: Also, the form would be dispersion-dependent
Is the averaged v_g more similar to the v_s
Density of states

## Slide 17
Dispersion Dependence
Point Defect:
Umklapp:
Quantity of interest:
Heat Capacity:
Phonon Density of States:
Gurunathan, R., Hanus, R., Dylla, M., Katre, A., Snyder, G.J. arXiv:1910.03654, 2019.
Notes: We can think about the regimes where this integral is separable such that the group velocities cancel out. That would be the regime in which grop velocity is fairly frequency independent, or when the coefficient a (representing the point defect scattering strength) is small. In these regime, we can justifiably reach the K;lemens expression without making any assumptions about dispersion relation. Suggesting that for many materials without the exotic phonon properties discussed at this conference, this expression remains predictive
Action item: try this before dft
What’s the significance? Mechanism for how the phonon structure dependence is softened. Mehcanism

## Slide 18
Phonon-Interface Scattering
Symmetric Twist Boundary
Semicoherent Heterointerface
Coherent Twin Boundary
𝜽
Notes: Whereas, the status quo models of point defect scattering are well-established and well-characterized, the current models of phonon –interface scattering do not get to the heart of the defect’s scattering potential. In this case, I will introduce our understanding of how to treat phonon scattering for these special, low energy grain boundaries commonly found in thermoelectric materials.

## Slide 19
What’s Missing in Boundary Scattering Models?
Hanus, R; Garg, A., Snyder. G.J. ,Commun. Phys. 1, 78 (2018).
(Snell’s Law) Acoustic Impedance Mismatch: Based on
Diffuse Mismatch: Based on
Frequency-dependent scattering that can explain the trend in 𝜅 in polycrystals
1
2
Symmetric Tilt Boundary
Notes: The two current standard models are based on the mismatch in the properties of the half crystals surrounding an interface. In one case, it is the mismatch in acoustic impedance or the mass density times average phonon velocity… and in the other instance it is the ratio of heat capacity weighted phonon velocities. Therefore, in both instances, the structure and properties of the interface, itself, are being ignored. However, in a paper recnelty out of our group, and quite familiar to several people in the room, the underlying dislocation structure of a symmetric tilt boundary was used to explain anomalous low –temperature thermal conductivity data. A crossover in the frequency dependence of the phonon relaxation time was discovered, where the long wavelength phonons view the boundary as a planar defect leading to a frequency-independent scattering while the short wavelength phonons resovle the underlying periodic dislocation array to yield a 1/ frequency dependence. This frequency-dependence could explain the anomalous T^2 thermal conductivity trend observed in polycrystalline materials. With this suggestion that the underlying dislocation nstructure matters in this process, we were then interested in evaluating scattering potentials of other special grain boundaries.
Label symmetric tilt boundary
Animate?

## Slide 20
Scattering Rate from Deformation at a Boundary
Deformation:
Strain tensor
Rotation tensor
Anharmonicity:
Anisotropy:
Crystallographic direction
Displacement
Real Space Strain Field
Real Space Strain Field
𝜖(𝒓)
Real Space Scattering Potential
Real Space Scattering Potential
𝑉(𝒓)
Scattering Matrix Element
Scattering Matrix Element
𝐶(𝒒)
𝒒=𝒌^′−𝒌
Notes: This slide covers some of the mechanics of the model. In large part, we start with the deformation around the grain aboundary, which can be used to determine the strain and rotation around the interface. As before with point defects, strain will couple to the phonon states via the anharmonicity captured by the gruneisen parameter. The rotation will couple through the anisotropy of the material. Or more specifically, the change in phonon velcoities with a change the crystal orientation. From these real space strain and rotation fields, we can calculate real space scattering potentials like the V’s shown here. A final Fourier transform yields the scattering matrix element, which can be used to compute the scattering rate.

## Slide 21
1D Array of Dislocations to 2D Grid
Hanus, R; Garg, A., Snyder. G.J. ,Commun. Phys. 1, 78 (2018).
m
n
﻿R A Brown 1983 J. Phys. C: Solid State Phys. 16 1009
Notes: The first case is that of a tilt grain boundary, which can be simply represented as an array of evenly spaced edge dislocations. And the slightly more complicated case we have recently focused on is the symmetric twist boundary case, where there is now two sets of evenly spaced screw dislocations with perdendicualr dislocations liens and burgers vectors. Our treatment starts with considering the deformation tensor. From this we can derive the symmetric strain tensor, where the materials characteristic determining the scattering strength of the strain field is the anharmonicity captured by the gruneisen parameter. The antisymmetric tensor captures the rotation, where the change in phono nfreuency with a rotation is determined by the anisotropy of the crystal. A good visual representation of this is the slowness plot which shows the variation of phonon velocity with a change in orientation. From this theory, we can derive similar scattering potentials and calculate a phonon relaxation time due to these various effects.
One complication when moving to the symmetric twist boundary and heterointerface is that there are two orthogonal dislocation arrays now forming a grid, which we can label the m and n array. Given the geometry of their respective strain fields, the scattering matrix element is as follows. The delta functions enforce that the strain fields scatter independently without any requirement to handle cross-terms.
Except the case of q_y = q_z = 0, but closer analysis shows that this either corresponds to a non-resistivie forward scattering process or a specular reflection due to the long-ranged misorientation at the interface, which can be handled separately.

## Slide 22
Twist Boundary: Misorientation is Pure Rotation
𝜽
Si- Si
﻿J H van der Merwe 1950 Proc. Phys. Soc. A 63 616
Notes: Moving onto some preiliminary calculations, here are the calculated relaxation times versus magnitude of the wavevector for the twist boundary, which can be decomposed into a grid of screw dislocations. Here the Peierls-nabarro strain fields around a screw dislocations are used to calculate the periodic strain fields shown here. But in this case, the rotation tensor at the interface is fully described by a misorientation angle, theta, which we will say proceeds as a step function change at the interface. These initial results suggest that tilt boundaries are more potent scatterers than twist boundaries, given their lower relaxation times. However, the exact mechanism of this is not known. Analyzing the long wavelength limit, which is determined by long range deformations at the boundary, we noticed that tilt boundary is fully determined by the rotation at the boundary, while long-ranged shear effects seem to persist in the twist boundary case.
Point out scales

## Slide 23
Semicoherent Heterointerface
Shear Stress at a Misfit Dislocation:
Yao Yugui, Tsuchiang Wang, and Chongyu Wang. Physical Review B, 59(12):8232–8236, 1999
﻿J H van der Merwe 1950 Proc. Phys. Soc. A 63 616
Notes: The next geometry we’re considering is the semicoherent heterointerface, or the interface between two materials with different lattice parameters, in which a grid of edge-like misfit dislocations form to alleviate coherency strain. This is a particularly important case in thermoelectric owing to the interest in the engineering of precipitates to lower thermal conductivity. The strain fields from the Van der Merwe model are plotted here for an example Si-Ge interface. A slice of the dilatational strain component is plotted here with a clear discontuinity interface, but primarily it shows that the dilation proceeds largely as a step function, basically a representation of the step function change in lattice parameter. So, in this case, we propose treating the periodic shear strain at the interface using the expression derived in this PRB paper, and treating any dilatational effects using an acoustic mismatch term.

## Slide 24
Coherent Twin Boundary: Acoustic Mismatch
Kim, K., Lee, J., Kim, B. et al. Nat Commun 7, 12449 (2016)
Acoustic Impedance:
Transmissivity:
Rotate:
Jaeken, J. and Cottenier, S., Computer Physics Communications 20 (2016).
Notes: Finally, our group became interested in the coherent twin boundary after a recent experimental investigation showed a correlation between thermal conductivity in Bismuth Telluride and the coherent twin density. As implied by the name, this boundary does not have dislocations or dangling bonds at the interface, but still comprise a rotation of the crystal. While it may be thought that there is no acoustic impedance at such a boundary because material 1 and 2 surrounding the interface, we applied the same argument of anisotropy to calculate a transmissivity based on the change in phonon velocity with change in orientation. These polar digrams show the direction-dependent phonon velocities for Bi2Te3 computed using the Christoffel package. By applying the 60 degree rotation of the twin boundary and computing the change in average phonon velocity, a transmissivity of 0.67 was calculated.While this requires further verification, it may point ot a large thermal resistance largely unexplored for coherent twin boundaries.

## Slide 25
Proposal Summary
Model the thermal resistance of interfaces by considering their specific structure in addition to their acoustic mismatch
1) Completion/Validation of Boundary Scattering Models
  Compare to experimental thermal boundary resistance measurements
2) Perform Calculations of Interfacial Strain Energy and full Grain Boundary Energy
Ju, S. and Liang, X. Journal of Applied Physics 113, 053513 (2013)
Xu, D., Hanus, R., Xiao, Y., et al. Materials Today Physics 6 (2018)
Notes: To summarize, the future steps involve completion and verification of the boundary models discussed. Verificiation, in part, is possible through an experimental collaborator at the University of Arizona who measures thermal boundary conductance at the interface of two bonded thin films. Additionally, I am interested in calculation the interfacial strain energy for each of these cases as a means to better understand the origin of their scattering potentials.
Highlight gaps in knowledge.

## Slide 26
Proposal Summary
Model the thermal resistance of interfaces by considering their specific structure in addition to their acoustic mismatch
1) Completion/Validation of Boundary Scattering Models
  Compare to experimental thermal boundary resistance measurements and molecular dynamics results
2) Perform Calculations of Interfacial Strain Energy
Ju, S. and Liang, X. Journal of Applied Physics 113, 053513 (2013)
Notes: To summarize, the future steps involve completion and verification of the boundary models discussed. Verificiation, in part, is possible through an experimental collaborator at the University of Arizona who measures thermal boundary conductance at the interface of two bonded thin films. Additionally, I am interested in calculation the interfacial strain energy for each of these cases as a means to better understand the origin of their scattering potentials.
Highlight gaps in knowledge.

## Slide 27
High-throughput Methods
StarryData2
HT DFT data
Thermoelectric metrics:
experimental
computational
Notes: Lastly, I will discuss a materials informatics project conducted in conjunction with Questek Innovations geared specifically at the prediction of good, thermoelectric materials, While the first phase of this work focused specifically on the properties of pure compounds, future trajectories are aimed at microstructural engineering and, therefore, tie back to the phono-defect interactions discussed earlier.

## Slide 28
Assessment of a Thermoelectric Material
Weighted Mobility
Combination of electronic structure descriptors that indicate how good of a power factor you can achieve
Lattice thermal conductivity
Heat carried by atomic vibrations in the lattice
Quality factor:
Doping level:
Kang, S. and Snyder, G.J. arxiv:1710.06896 (2017)
Notes: The efficiency of a thermoelectric device is directly related to its figure of merit zT, which, in turn, is calculated form compoenents: S, sigma, and kappa. As shown in this diagram, however, each of these material properties are highly dependent on doping, which in semiconductor processing, is often controlled extrinsically. Therefore, assessing the intrinsic potential of a thermoelectric is non-trivial from zT alone. The solution is to perform what’s known as quality factor analysis. The quality factor is diretly related to the ceiling value n the zT if the material is optimally doped. And it is the ratio of weighted mobility, which combines electronic structure descriptors related to thermoelectric potential to the lattice thermal conductivity. Essentially, so far, we have abuilt a databse, which combines experimental and computational data and performed quality factor analysis on each entry…. Creating the largest databse of quality factors and weighted mobilities to date. The next couple slides will briefly cover some of the analysis steps.

## Slide 29
Experimental Pathway: Single Parabolic Band
StarryData2: Digitized plots from over 4,000 publications on thermoelectric materials, mainly of vs. T
B
Kang, S. and Snyder, G.J. arxiv:1710.06896 (2017)
Notes: The experimental data came from the sTarrydata2 databse with data from over 4,000 publications on thermoelectric. Typically, plots of Seebeck coefficient, electrical conductivity, and thermal conductivity versus temperature were provided. Here, we will assume conduction from a single, free-electron-like parabolic band, which can be doped into as shown. Under this approximation, the relation between the Seebeck coefficient and the electrical conductivity can be used to compute the transport function, which characterizes the conductivity quality of a band at a particular doping level. The transport function is used to calculate wighted mobility at a given at a given temperature and the lattice thermal conductivity can be computed from the total by simply subtracting off the electronic contribution to yield the final quality factor.

## Slide 30
Computational Pathway: BoltzTraP Effective Mass
Pros: Need not make the approximation of a single, parabolic band
Cons: Relaxation time () is not easily accessible
BoltzTraP: interpolate bands to calculate gradients/slopes
and
Acoustic Optical
MPContribs Carrier Transport Database
Ricci, F., Chen, W., Aydemir, U. et al. Sci Data 4, 170085 (2017)
Huck, P., Gunter, D., Choila, S., et al. Currency and Computation 28 (2019)
Yan, J., Gorai, P., Ortiz, B. et al. Energy Environ. Sci., 2015,8, 983-994
Notes: Starting from DFT structures has its pros and cons. For one, the single parabolic band assumption is no logner required b/c we have access to the full complexity of the electronic structure. However, in this case, the relaxation time is less accessible. The Carrier Transport database accessible through Materials Project uses the BoltzTraP method of band interpolation to calculate transport coefficeints like Seebeck and conductivity. However, this is at a constant relaxation time, and specific doping level. We apply an effective mass model to compute a Seebeck and conductivity effective mass from these quantites that is more agnostic to doping level and relaxation time. In the case of conductivity, this is easily understood as a rearrangement of the Drude model. In the case of thermal conductivity, phonon velocities are calculated from DFT elastic constants. A semi-empirical model of thermal conductivity is used, where the acoustic branch of phonons is treated as phonon-like, with a relaxation time limited by phonon-phonon interactions while the optical branch is treated as Einstein-like modes or couples, local oscillations.
Animate

## Slide 31
Proposal Summary
To Date: Largest Consolidated Database of Thermoelectric Quality Factor
1) Use Clustering Analysis, Dimensionality Reduction, and Regression Techniques to Expose Underlying Patterns/Groupings in the Database
Notes: To date, there is this consolidated database of thermoelectric quality factors. Our first proposal is to analyze the data using techniques of clustering and dimensionality reduction. This provides a way to visualize similarities and groupings in the database, in the case wehre each sample is described by numerous features. This is a first cursory attempt using k-means clustering and principal component analysis. The clusters are labelled with the mean value of weighted mobiloity and quality factor, and do appear to show specific pockets of primising thermoelectric materials.
Add factor loadings

## Slide 32
Proposal Summary
To Date: Predictions of pure compounds for thermoelectrics
2) Build microstructural models using CALPHAD (Calculation of Phase Diagrams) and mechanistic models and combine with interfacial thermal models
Peters, M. Retrieved from ProQuest Dissertations Publishing (2018).
Notes: As mentioned, the databse so far is good for the selection of a pure thermoelectric ompund. These are some novel or only recently investigated thermoelectric ompounds identified as having high quality factor or high weighted mobility. However, it does not yet include the impact that alloying or microstructure can play. Therefore, we propose, once again in conjunction with Questek innovations, to build microstructure prediction models using CALPHAD and other tools, which can be paired with the interfacial thermal models discussed previously

## Slide 33
Conclusion and Acknowledgements
Broad Goal:
Study phonon-defect interactions using the tools of perturbation theory and continuum elasticity theory
Apply models in the context of real materials
Proposal:
Further development of physics-based models of phonon-interface scattering
Notes: So, thank you for your time. To summarize, my proposed thesis work takes on the broad goal of understanding phonon-defect interactions using conventional theories and approximations, and applying these models to understand real materials, specifically in the application of thermoelectric, which is the bread-and-butter of our research group. The remainder of my proposed work will be more focused on the problem of phonon-interace scattering, which is highly relevant to the modern age of thermoelectric research that is finally looking into the impact of microstructure.

## Slide 34
Extra Slides

## Slide 36
Proposal Summary
To Date: Largest Consolidated Database of Thermoelectric Quality Factor
1) Use Clustering Analysis, Dimensionality Reduction, and Regression Techniques to Expose Underlying Patterns/Groupings in the Database
PC1
PC2
Notes: To date, there is this consolidated database of thermoelectric quality factors. Our first proposal is to analyze the data using techniques of clustering and dimensionality reduction. This provides a way to visualize similarities and groupings in the database, in the case wehre each sample is described by numerous features. This is a first cursory attempt using k-means clustering and principal component analysis. The clusters are labelled with the mean value of weighted mobiloity and quality factor, and do appear to show specific pockets of primising thermoelectric materials.
Can maybe make this table better?
Add factor loadings… maybe get rid of?

## Slide 37
MagicMat Example Entry:
Kang and Snyder . https://arxiv.org/abs/1710.06896 (2017)

## Slide 38
Phonons as Plane Wave Solutions in a Harmonic Solid
Riley’s Thesis
Harmonic…
Plane wave…
Solutions to equations of motion…
https://henriquemiranda.github.io/phononwebsite/phonon.html
Notes: Include phonons gif

## Slide 39
Unit Cell versus Atomically Average Quantities
Unit Cell Microstates
Atomic Microstates
Notes: So, I decided to extend each of these models and come up with a scattering parameter Gamma using a sort statistical mechanics approach.

## Slide 40
Dispersion Dependence
Analytical Umklapp:
Joint Phonon Density of States:
Togo, A., Chaput, L., Tanaka, I., Phys. Rev. B. 91 (2015).
derives frequency dependence from joint density of states
Notes: This finding remains consistent with recent high- throughout computational studies enables by new thermal transport codes like almaBTE and phono3py. In a study by Atsushi Togo, he demonstrated through a scan of about 100 cubic compounds that the scattering rate of for phonons derives its frequency dependence from the joint density of states
An expression of the joint density of states is shown here, and conceptually, it counts all the possible phonon processes, taking into consideration the conservation of momentum and energy
We can think about the regimes where this integral is separable such that the group velocities cancel out. That would be the regime in which grop velocity is fairly frequency independent, or when the coefficient a (representing the point defect scattering strength) is small. In these regime, we can justifiably reach the K;lemens expression without making any assumptions about dispersion relation. Suggesting that for many materials without the exotic phonon properties discussed at this conference, this expression remains predictive
Make the JDOS graphs better. Think about whether to include this slide, generally

## Slide 41
Dimensionality crossover
Hanus, R; Garg, A., Snyder. G.J. ,Commun. Phys. 1, 78 (2018).
Notes: The early motivation for looking into this problem was this interesting finding in the low temperature thermal conductivity trends where boundary scattering may dominate. As shown here, for polycrystalline materials, the thermal conductivity versus temperature relation showed a T^2 dependence, which deviated from the T^3 dependence observed for single crystal materials. Most theories suggested for phonon scattering due to planar defects

## Slide 42
BoltzTraP
,
Electron
bandstructure
Phonon
bandstructure
HT-DFT: m* from BoltzTraP and from Elastic Tensor
MPContribs
Materials Project
Notes: zT versus temperature: https://www.researchgate.net/figure/Thermoelectric-figure-of-merit-zT-as-a-function-of-temperature-for-thermoelectric_fig3_329227296

## Slide 43
Dispersion Dependence
Notes: Remove math?? Leave this in at all??
Plot frequency dependence of the vg^3 for BvK

## Slide 44
StarryData2: Quality Factor from S vs. σ Relation
Analysis Steps:
Use S vs. relation to compute weighted mobility:
Calculate by subtracting off electronic portion ()
Calculate quality factor:
Kang and Snyder . https://arxiv.org/abs/1710.06896 (2017)
Digitized plots from over 4,000
publications on thermoelectric materials
Notes: Beautify!!

## Slide 45
1D Array of Dislocations to 2D Grid
Hanus, R; Garg, A., Snyder. G.J. ,Commun. Phys. 1, 78 (2018).
m
n
k
k’
k’
k
Notes: The first case is that of a tilt grain boundary, which can be simply represented as an array of evenly spaced edge dislocations. And the slightly more complicated case we have recently focused on is the symmetric twist boundary case, where there is now two sets of evenly spaced screw dislocations with perdendicualr dislocations liens and burgers vectors. Our treatment starts with considering the deformation tensor. From this we can derive the symmetric strain tensor, where the materials characteristic determining the scattering strength of the strain field is the anharmonicity captured by the gruneisen parameter. The antisymmetric tensor captures the rotation, where the change in phono nfreuency with a rotation is determined by the anisotropy of the crystal. A good visual representation of this is the slowness plot which shows the variation of phonon velocity with a change in orientation. From this theory, we can derive similar scattering potentials and calculate a phonon relaxation time due to these various effects.
One complication when moving to the symmetric twist boundary and heterointerface is that there are two orthogonal dislocation arrays now forming a grid, which we can label the m and n array. Given the geometry of their respective strain fields, the scattering matrix element is as follows. The delta functions enforce that the strain fields scatter independently without any requirement to handle cross-terms.
Except the case of q_y = q_z = 0, but closer analysis shows that this either corresponds to a non-resistivie forward scattering process or a specular reflection due to the long-ranged misorientation at the interface, which can be handled separately.

## Slide 46
Closed Form Solutions for Point Defect Scattering are more predictive than might be expected
Debye Approximation
Slack, G. A.Phys. Rev. 126, (1962).

## Slide 47
Dispersion Dependence
M. T. Agne, R. Hanus, and G. J. Snyder, Energy Environ. Sci., 11 (13) 609–616, 2018.
M. Schrade and T. G. Finstad, Phys. Status Solidi, 1800208, 1–6, 2018.
Notes: Constant values for the kappaL/kappa0  justifying that the shapes are the same

## Slide 48
MLA: Per Primitive Unit Cell
The various primitive unit cells in the lattice are your “microstates”
V0 is the primitive unit cell volume
Notes: Suggestion in the skutterudite paper
… look at Klemens stuff and figure out how to talk about defect clusters

## Slide 49
MLA: Per Primitive Unit Cell
The various primitive unit cells in the lattice are your “microstates”
V0 is the primitive unit cell volume
Notes: Suggestion in the skutterudite paper
… look at Klemens stuff and figure out how to talk about defect clusters